04/21/2025

602-14.docx

## Section 602. — CULVERTS AND DRAINS

Material

Use on all projects when heat fusion welding HDPE pipe for lining culverts is used on the project or when constructing long rundown structures.

**602.02** Add the following:

Heat fusion welded thick-walled high density polyethylene (HDPE) pipe 708.10

Construction Requirements

**602.03 General**. Add the following:

Furnish heat fusion welded HDPE pipe with a rating of DR 21, 100 psi or higher. Heat fuse pipe according to ASTM F2620.