02/25/2025

Include if project has drilled shafts.

## Section 565. — DRILLED SHAFTS

**565.08 Concrete for Drilled Shafts.** Delete Table 565-4 and substitute the following:

**Table 565-4**

**Concrete for Drilled Shafts**

|  |  |  |
| --- | --- | --- |
| **Method** | **Class** | **Slump** |
| Shafts constructed without drilling fluid | C(1) | 7±1 inches |
| Shafts constructed with drilling fluid | C(1) | 8±1 inches |
| Shafts for underwater placement | S | – |

(1) Use Class C(AE) concrete on portions of the drilled shaft above the finished ground-line unless otherwise noted.