INCLUDE SECTION 552 AS NEEDED BASED ON CLAUSE INSTRUCTIONS

$$552.00A

Section 552. — STRUCTURAL CONCRETE

Revised 15 December 2025

INCLUDE CLAUSES $$552.03A, $$552.03B AND $$552.03C ON ALL PROJECTS WITH STRUCTURAL CONCRETE WORK

$$552.03A

552.03(a)(12)(c).  Delete the last sentence and substitute the following:

Include the design discharge time shown in Table 552-4.

$$552.03B

552.03(a).  Delete Subsection (17) and substitute the following:

(17) Reserved.

$$552.03C

552.03(a).  Delete Subsection (23) and substitute the following:

(23) Specified design strength and required average strength (f'cr) for the concrete mixture at 28 days as determined by the process described in Section 4 of ACI 301. This process and associated calculations are outlined on Form FHWA 1608. Pending 28-day strength results, a mix design may be approved on the basis that 7-day compressive strength results are at least 85 percent of the required average strength (f'cr) at 28 days;