INCLUDE SECTION 701 AS NEEDED BASED ON CLAUSE INSTRUCTIONS

##701.00A

Section 701. — CEMENTITIOUS MATERIAL

Revised 27 January 2026

INCLUDE THE FOLLOWING ON ALL PROJECTS WITH MORTAR

##701.05A

701.05(b).  Delete Subsection (2) and substitute the following:

(2) Length change, ASTM C157, except cure according to		   0.07 percent maximum

ASTM C928 when using rapid hardening mortar