## Section 501. — MINOR CONCRETE PAVEMENT

01 APR 2025 – FP-24

Construction Requirements

WFL Specification 01 APR 2025 5010010

Include the following when work is required under this Section.

**501.03 Composition (Concrete Mix Design).**

Delete the second sentence of the first paragraph and substitute the following:

Submit concrete mix designs for approval on Form FHWA 1606, *Minor Portland Cement Concrete Mix Design*, at least 30 days before production.

WFL Specification 01 APR 2024 5010020

Include the following when compressive strength cylinders are required.

### 501.06A Sampling.

(Added Subsection).

Take samples for compressive strength according to Table 501-2. Provide the appropriate initial curing of concrete cylinders taken for compressive strength testing and transport the cylinders to the project curing facility.

Provide suitable containers to protect and continue the curing of cylinders while transporting. Deliver cylinders to the Vancouver Laboratory according to Subsection 154.03. Cylinders will be tested at 7, 14, and 28 days from the date molded. Ensure cylinders arrive at the Vancouver Laboratory at least 1 business day before the designated test date.

### 501.14 Acceptance.

Add the following to Table 501-2 Note (4):

Transportation of specimens to laboratory may exceed time limits specified in AASHTO T 23.